PELLASAN SXL Fatliquor for enhanced softness

| Characteristic | mixture of special anionic and non-ionic, sulfited natural components |
| --- | --- |
| Appearance Concentration | brown liquid 85% ± 2 ISO 760 |
| pH Value: | 8.4 ± 0.5 (1:10 ) DIN 53 345 |
| Ionity | anionic |
| Light Fastness* | 4 - 5 DIN 54 004 |
| Preparation | Stir well before use; Emulsify with water at 50°C |
| Storage Stability (Months) | 12 |
| Field of Application | - used in fatliquoring for all types of soft leathers, garments, gloves, shoe napa, upholstery and car-upholstery - can be used in pickle, tanning and main fatliquoring |
| Properties | - enhanced softness - humidity retaining substances guaranteeing humidity equilibration even in fast drying process - warm lively touch of the leather - very good fogging performance - product stable to pickle and chrome |
| Application | - can be used in pickle, tanning and main fatliquoring |
| Storage Behavior | - it is viscous below + 5 °C but regains its normal aspect at room temperature |