PELLASAN 64

Electrolyte stable special fatliquoring, AOX free

| Characteristic | mixture of anionic and nonionic fatliquors with stabilisers |
| --- | --- |
| Appearance | yellowish, liquid |
| Concentration | 50%+2 ISO760 |
| pH Value: | 7.8 + 0.3 (1:10 ) ISO 4316-1977 |
| Ionity | anionic |
| Light Fastness* | 5 + DIN 54 004 |
| Heat Yellowing* | DIN 54 001 |
|  | 70℃ / 72 h | 4,5 + |
|  | 100℃ / 144h | 4 + |
|  | 135℃ / 1h | 4,5 + |
| Preparation | it can be applied into the float withour pre-emulsion |
| Storage Stability (Months) | 12 |
| Field of Application | - alone or combined with anionic/nonionic fatliquors for all kinds of leather - special developped for car seat, furniture, garment leather and double face |
| Properties | - fluffy, soft and velvet-like touch - uniform penetration of fat - good binding to the leather fibre, which is stable to dry cleaning - it is a modern, highly electrolyte stable fatliquoring agent for fur which meets highest technical requirements - it is highly light fast and has a very good stability to heat agein - good distribution of natural fat substances - very uniform dyeing - AOX free, easy biodegradable |
| Application | - in pickle 1-6% based on pelt weight - in chrome tannage 1-6% based on pelt weight - in retannage 2-8% based on shaved weight in licker float for stabilisation 10-30% of total amount of fat |